## Slide 1
Nanosensor Research at FSU
Zhiping Luo, Daryush Ila
FSU IMREL
1. Rare-earth (RE3+) codoped BaSiF6 and BaGeF6 nanowires
  Synthesis of BaSiF6 and BaGeF6 nanowires
  Characterization by photoluminescence (PL) and cathodoluminescence (CL)
  Fast luminescence property
  Application of BaGeF6 nanowires in H2O2 sensing
2. Rare earth (RE3+) doped BaWO4 nanofibers
  Fabrication of porous nanofibers through electrospinning
  Characterization by PL and CL
  Application in highly sensitive explosive detection

## Slide 2
FSU IMREL
Research Capacity at FSU
JXA-8530F EPMA at FSU (indicated are CL funded by NSF MRI).
The Electron Probe Microanalyzer (EPMA) was funded by ARO in $1.4M in 2009;
The new EDS detector for chemical analysis was funded by ARO in $54K in 2015;
The cathodoluminescence was funded by NSF MRI program in $201K in 2016;
The EPMA instrument at FSU is the unique instrument with field-emission source in North Carolina and neighboring states.

## Slide 3
FSU IMREL
BaSiF6 Nanowires
(d)
Superlong BaSiF6 nanowires are synthesized (35.8 nm in diameter and 10–50 m in length);
Strong emissions are obtained in PL and CL;
The decay time shows subnanosecond fast luminescence property.
G. George et al., J. Mater. Chem. C 6, 7285–7294 (2018).
1 m
Photoluminescence (PL)
Cathodoluminescence (CL)
Decay time

## Slide 4
FSU IMREL
BaGeF6 Nanowires
(d)
Superlong BaGeF6 nanowires are synthesized (58 nm in diameter and 50–100 m in length);
Strong emissions are obtained;
The BaGeF6 nanowires can be used as luminescence probe for sensitive detection of H2O2 (25 ppm).
G. George et al., RSC Adv. 8, 39296-39306 (2018).
Photoluminescence
10 m
Sensitive detection of H2O2
H2O2 Detection

## Slide 5
FSU IMREL
BaWO4 Nanofibers
(d)
BaWO4 nanofibers were synthesized by electrospinning;
Highly selective towards aromatic nitro-compounds and H2O2, with the sensitivity within the range of 1–400 ppb and 1–10 ppm, respectively.
G. George et al., J. Mater. Chem. C 7, 14949–14961 (2019).
Mechanism
Sensitivity
Detection

## Slide 6
Group Members
FSU IMREL
Dr. Gibin George
Postdoc Fellow
Candyce
Collins
Caressia
Edwards
Jessa
Guffie
Carlos
Posada
Lenore
Miller
Aspyne
Silvestro
Dr. Zhiping Luo
Project PI
Dr. Daryush Ila
Co-PI
Jacob Hayes
Dr. Sivasankara Ede
Postdoc Fellow